Multi-scale Modeling and Simulation in Solid Mechanics

ME417

Instructors: Prof. Wing Kam Liu

Course Objectives:

- Understand the underlying principles of molecular dynamics (equations of motion for atoms, atomic interactions).

- Gain proficiency in designing molecular dynamics simulations using available software (LAMMPS).

- Understand the connection between information available on small (atomistic) and large (continuum) scales.

- Applications

  - Nanostructure materials: Nanowires: single crystal Si;  Nano Carbons: nanotube

  - Polymer nano-composite: polymer mechanics, polymer and polymer-fillers modeling, Multi-scale modeling (MD, Continuum)

Homework

There will be two homework assignments during the term. The purpose of the homework is to provide the students with an opportunity to apply theoretical and computational concepts to multi-scale problems.

Projects

Projects typically include a multi-scale simulation aspect and some preliminary theoretical concepts on the expected observations. There will be one midterm project and one final project.  Topic of midterm project:  nanowire (MD).  Topic for the final project : students will have the opportunity to apply the concepts that they have learned in class to a research problem of their own interest.

Grading

Homework (30%), Midterm project (30%), Final project (30%), Participation (10%)

Textbook

There is no required textbook. Some resources relevant to this class are provided below:

• Liu, Wing Kam, Karpov, Eduard G., and Park. Harold S., Nano Mechanics and Materials: Theory,

Multiscale Methods and Applications. John Wiley & Sons, Ltd, 2006.

• Schroeder, Daniel V. An Introduction to Thermal Physics. Addison Wesley Longman, 1999.

• Fish, Jacob and Belytschko, Ted,  A First Course in Finite Elements. John Wiley & Sons, Ltd, 2007.

• Belytschko, Ted, Liu, Wing Kam, and Moran, Brian, Nonlinear Finite Elements for Continua and

Structures. John Wiley & Sons, Ltd, 2000.

Software: LAMMPS and ABAQUS will be used for the simulations.

Lab session will be held on Wed (if needed) or mutually agreeable time

Class Schedule

| Date |  | Topic | Detail description |
| --- | --- | --- | --- |
| Week #1 T: | Molecular dynamics | Introduction to Multiscale Simulations |  |
| Week #1 W: |  | LAMMPS Tutorial | LAB |
| Week #1 Th: |  | Introduction to MD I | Atomic structure and interatomic bonding |
| Week #2 T: |  | Introduction to MD II | Hamiltonian, Lagrangian Mechnics |
| Week #2 W: |  | LAMMPS Tutorial | LAB |
| Week #2 Th: |  | Thermodynamics I | Partition function |
| Week #3 T: |  | Thermodynamics II | HW#1 Due |
| Week #3 W: |  | LAMMPS Tutorial | LAMMPS Post-Processing |
| Week #3 Th: |  | Nanostructure |  |
| Week #4 T: |  | Lattice Mechanics I |  |
| Week #4 W: |  | LAMMPS Tutorial |  |
| Week #4 Th: |  | Lattice Mechanics II | HW#2 Due |
| Week #5 T: |  | Midterm Presentation |  |
| Week #5 W: |  | ABAQUS Tutorial |  |
| Week #5 Th: | Continuum and Bridging scale | Introduction FEM I |  |
| Week #6 T: |  | Introduction FEM II |  |
| Week #6 W: |  | ABAQUS Tutorial |  |
| Week #6 Th: |  | Bridging scale method I |  |
| Week #7 T: |  | Bridging scale method II |  |
| Week #7 W: |  | ABAQUS tutorial |  |
| Week #7 Th: |  | Cauchy-Born |  |
| Week #8 T: | Polymer composite | Introduction to Polymer | Viscoelasticity |
| Week #8 W: |  | ABAQUS tutorial |  |
| Week #8 Th: |  | Polymer mechanics |  |
| Week #9 T: |  | Polymer coarse grain MD |  |
| Week #9 W: |  | Project Discussion |  |
| Week #9 Th: |  | Polymer composite MD |  |
| Week #10 T: |  | FEM simulation of polymer composite |  |
| Week #10 W: |  | Project Discussion |  |
| Week #10 Th |  | Course wrap-up |  |

Module1: Introduction (4.5wks)

A.  Introduction_MD (1.5wk)

1. Why multi-scale modeling?

2. Lagrangian and Hamiltonian equations of motion

3. Interatomic potentials

  - Particle dynamics (Multi-body interaction) using interatomic potential

4. Algorithms, Periodic Boundary Condition

B. Thermodynamics (1 wk)

1. First and second law of thermodynamics, Entropy

2. Statistical ensembles: NVE, NVT, NPT

3. Free energy, Enthalpy,

C. Nanostructure (0.5 wk)

1. Nanowire: Single crystal silicon

2. Nano carbon:  Nanotube

C. Lattice Mechanics(1 wk)

1. Regular lattice structure

2. Equation of motion

Module2:  Continuum mechanics and Bridging scale (2.5 wk)

- Introduction to FEM (1wk)

- Bridging scale method (1wk)

  - Learn how to bridge two scales (MD and FEM)

- Cauchy-Born : Linking MD and FEM

  - Calculation of FEM stress from MD potential

Module3:  Polymer Nanocomposite (2.5wks)

- Introduction Polymer

- Molecular modeling and simulation of polymer

- Force field for polymer

- Mechanics of polymer and composite (Continuum modeling)

- Viscoelasticity, Creep, Stress relaxation, DMA test, Time-temperature superposition

- Coarse graining molecular dynamics of polymer composite

- FEM simulation of polymer composite